Product	Name	Organoid® ROSENBLÜTEN on flax backing	
	Article number	ROABLI0085FVPST	
Producer	Address	ORGANOID® TECHNOLOGIES GMBH
Nesselgarten 422 / Top 5
A-6500 Fließ
Austria
	
Description and applications	Name	Organoid® ROSENBLÜTEN on flax backing	
	Description	Natural plant material in full coverage on natural non-woven flax backing produced climate neutral in Tyrol	
	Applications	As wallpaper  
As a compound in wood-working
	
Plant material and density	Plant material	Fragrant red rose petals
	
	Density	Premium, full coverage	
Size and weight	Size	1 360 mm by 2 950 mm	
	Thickness	1.2 mm	
	Weight	590 g/m²
	
Product requirements	Food-safety	Binding agent safe for usage in contact with food in accordance with EU-regulation 1935/2004
	
Backing material	Material	Natural, non-woven flax fleece	
	Properties	Unbleached and breathable
from a renewable material
Contains 100% flax	
		Certified OEKO-TEX 100
Tensile strength in accordance with ISO 9073-3:
MD N/5cm 65
CD N/5cm 45
	
Technical implementation	Cut	Use scissors, a cutter or a plotter	
	Edges	Allow for imperfections 1-2 mm around 
the edges	
	How to install	As wallpaper:
•	Wall-pasting technique: Apply glue directly on the wall, apply wallpaper vertically and press on using a rubber roller
•	Double cut: Each panel overlaps with the one next to it (approx. 2 cm) 
•	Free match: The naturally scattered materials do not require matching patterns between panels

As a compound in wood-working
•	Process with normal wood-working machinery
•	Glue (e.g. white glue) is applied onto the wooden materials, as the fleece absorbs moisture and glue stains may appear on the front if glue is applied to the fleece
•	Cover the natural surface with the enclosed separating paper
•	Guidelines:
Max. pressing temperature. 60°C
Max. pressure 1 kg/cm²
Glue application: approx. 100 g/m²
Pressing time: approx. 15 minutes

Pre-trials and tests are recommended
	
	Glue recommendations	As wallpaper: Glutolin ECC extra clear
As a compound in wood-working: White glue
	
	Pay attention to	Surface must be clean, dry, weight-bearing, evenly absorbent, smooth, dust-free and neutral in colour. Recently plastered walls must be fully dried. Highly absorbent walls must be prepared with a suitable base. 

For sensitive wood-working applications, use a counter-balance (enclosed on request). Symmetrical construction is recommended, which means using the same surface on the front and back side.

Differences in colour can occur in different batches, this has to be taken into account when ordering multiple decks

Acclimatisation of Organoid natural surfaces: 
•	Bring product to room temperature before unpacking 
•	Store product protected from light, at about 20°C and 30-60 % relative humidity.

Storage:
•	Rolled goods: hanging system (e.g. paternoster)
•	Single panels: horizontal position (e.g. drawer system)	
	Processing guidelines available at:	www.organoids.com/en/installation-technical-implementation